NS 1.011.015

Specification for

VT D

| Product | Engineering | Project | Quality |
| --- | --- | --- | --- |
| Manager | Manager | Manager | Manager |
| A.Jamard | M.Emin | JP.Schultze | M.de Rycke |

NS 1.011.015  - Page 2/5

1. 	Scope

This specification applies to a Nickel-Cadmium cylindrical rechargeable single cell which SAFT designation is VT D. This cell belongs to the SAFT High temperature Ni-Cd cell series.

It means it has been designed for permanent charge applications at high temperature.

2.	Reference documents

IEC 285 : 1993 + Amendment 1/1995 Sealed Ni-Cd cylindrical rechargeable single cells. (Refer to items especially dedicated to cells for permanent charge at elevated temperatures).

3. 	General electrical specification

| Item | Specification | Units | Notes |
| --- | --- | --- | --- |
| SAFT cell designation | VT D |  |  |
| IEC cell designation | KRMT 35/62 |  |  |
| Nominal voltage | 1.2 | Volt |  |
| Rated capacity | 4000 | mAh | at 0.2C |
| Typical impedance | 7.0 | mOhms | at 1000 Hz |
| Charge current |  |  |  |
| Permanent | 200 | mA | 0.05 C |
| Normal | 400 | mA | 0.1 C |
| Charge duration |  |  |  |
| Normal | 16 | Hours |  |
| Peak Voltage in charge |  |  |  |
| Normal | 1.50 / 1.70 | Volt |  |
| Maximum continous |  |  |  |
| Discharge current | 20.0 | A |  |
| Temperature range |  |  |  |
| In permanent charge (recommended) | +15 to +45 | °C |  |
| In permanent charge (authorized maximum) | 0 to +65 | °C | Short duration < 1 month |
| In discharge | -20 to +65 | °C |  |
| In recommended storage | +5 to +25 | °C |  |
| In extended storage | -40 to +65 | °C | short duration < 1 month |

NS 1.011.015  - Page 3/5

4. 	General mechanical specification

| Bare Cell Drawing (mm) | Bare Cell Dimensions |
| --- | --- |
|  | Maximum Diameter (mm) : 32.3 |
|  | Maximum Height (mm) : 60.30 |
|  | Positive contact |
|  | Diameter (mm) : 5.6 |
|  | Overstep (mm) : 3.5 |
|  | Typical Weight (g) : 132 |

5. 	Capacity

5.1	IEC Capacity

IEC capacity is rated as follows :

	Temperature 			: 	+20° ± 5°C

	Constant charge current 	: 	0.1C = 400 mA constant current

	Charge duration 		:	16 hours

	Period of rest after charge	:	1 to 4 hours

	Discharge constant current	:	0.2C = 800 mA constant current

The operating time until the voltage drops to 1.0 volt/cell must not be less than 300 minutes - 
2 cycles are permitted.

The IEC capacity is then minimum 4.0 Ah.

5.2	Available capacity

The following cross table gives Minimum Available Capacities of a multi-VT D battery under various charge and discharge conditions. The temperature is +20°± 5°C, the battery being initially fully charged. Deviation depending on test conditions may be observed.

NS 1.011.015  - Page 4/5

| # CHARGE |  | PERMANENT | NORMAL |
| --- | --- | --- | --- |
| Rate |  | 0.05C | 0.1C |
| Current (mA) | (mA) | 200 | 400 |
| Duration (hour) | (hour) | > 48 | 16 |
| Rest after charge | (hour) | No rest | 1 |
| DISCHARGE (*) |  | CAPACITY (Ah) | CAPACITY (Ah) |
| Rate | Current (A) |  |  |
| 0.2C | 0.8 | 4.0 | 4.0 |
| C | 4.0 | 3.60 | 3.60 |
| ## 3C | 12.0 | 2.8 | 2.8 |

(*) up to an end of discharge voltage of 1 V / cell.

6.	Charge

6.1	Permanent charge

The multi-VT D battery is designed to be permanently charged between +15°C to +45°C with above mentionned constant current (0.05C).

Occasional temperature (0 to +65°C) is accepted for short duration only (< 1 month).

For a usage at temperature lower than 0°C it is mandatory to limit the charge voltage at 1.55V per cell. In case of charge with a multi-rate current, or pulsed charge, multi-VT D battery must be charged at a minimum « trickle charge rate » of 0.033C between  the pulses.

7.	Temperature characteristics

The following table gives the Minimum Available Capacity of a multi-VT D battery under various discharge rate and temperature and after the following charge conditions :

	Normal charge : 0.1C charge current for 16 hours

	Temperature of discharge : +20°C ± 5°C

	Maximum rest after charge : 4 hours at temperature of discharge

Capacities (Ah) are given for a final discharge voltage of 1 volt/cell. Deviation depending on test conditions may be observed.

### NS 1.011.015 – Page 5/5

| ##### TEMPERATURE | #### RATE OF DISCHARGE |  |  |  |
| --- | --- | --- | --- | --- |
| ##### OF DISCHARGE | 0.2C = 800mA |  | 0.5C = 2.0A | ###### C = 4.0A |
| +40°C | 3.8 | 3.5 |  | 3.1 |
| +20°C | 4.0 | 3.8 |  | 3.6 |
| 0°C | 3.4 | 3.0 |  | 2.8 |
| -20°C | 2.3 | 1.7 |  | - |

8.	Charge retention

After a 28-day storage at +20°C ± 5°C the multi-VT D battery shall retain typically 85% of its rated capacity, the battery being fully charged. After a 7-day storage at +40°C ± 5°C the multi-VT D battery shall retain typically 90% of its rated capacity, the battery being fully charged initially.

- Storage

SAFT recommends to store the battery within the temperature range at +5°C to +25°C in a 65% ± 5% Relative Humidity room in a dishcarged state with open circuit. An extended storage within -40°C to +60°C temperature range and 65% ± 20% Relative Humidity room is permitted.

- Overcharge

After a 3 month continuous charge at 0.1C = 400 mA at +40°C ± 5°C, the capacity at 0.2C discharge rate of a multi VT D battery at 1.0V / cell is typically 3.7Ah.

- Life duration in permanent charge application

Life duration of a multi-VT D battery depends mainly on cell / battery temperature and overcharged capacity.

The end life of the multi- VT D battery is reached when the battery capacity drops down to 60% of the initial capacity.

Typical life of a multi-VT D battery is 4 years  with the average operating conditions :

 	working battery temperature 		+40°C

 	permanent charge current		0.05C

 	1 or 2 discharges per month at 0.5C discharge rate